370 TRADITIONAL ALUMINIUM PIPEWORK FOR EXTERNAL USE:

Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,
 Elms Farm Industrial Estate, Bedford MK41 0LZ
 Tel: 01234 359438, Fax: 01234 357199.
 Email: enquiries@marleyalutec.co.uk

Reference: Traditional square aluminium rainwater system to BS8530.

Accessories: Bends, Branches, Access Pipes, 2 Piece Offset, Shoes, Hopper Head, Pipe Clips
Size: 102x102mm
Type / grade: Marine Grade extruded aluminium to BS EN755-2:2008 grade 6063-T5 pipe

with cast aluminium sockets to BS EN 1706:2010

Finish: Polyester powder coated to BS EN 12206-1:2004 or Mill Finish (bare aluminium) (Delete as appropriate)
 Colour: From manufacturer’s standard range TBC
Functional life expectancy: 50 years

Fixing: Via eared cast sockets and or extruded pipe clips. Plug and screw to wall with Alutec 50mm x No. 16 domehead screws.

Jointing: Cast sockets sealed with Alutec sealant allowing for a 3-4 mm vertical thermal movement gap.