**F30 ACCESSORIES/SUNDRY ITEMS FOR BRICK/BLOCK/STONE WALLING**

**PRODUCTS**

EVOKE ALUMINIUM COPING SYSTEM

780 Coping

Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,  
 Elms Farm Industrial Estate, Bedford MK41 0LZ  
 Tel: 01234 359438, Fax: 01234 357199.  
 Email: enquiries@marleyalutec.co.uk  
 Reference: Aluminium coping system  
 Size: To be determined TBC   
 Type / grade: 2mm thick aluminium sheet (upto 400mm span), 3mm thick aluminium (over 400mm span).

Finish: Polyester powder coated to BS EN 12206-1  
 Colour: From manufacturer’s standard range TBC  
 Functional life expectancy: 50 years

Wind loading – Designed to withstand hurricane force winds upto 176 mph

Fire resistance: A2-s1, d0 unlimited use

Jointing: Internal jointing – Weather tight butyl seal

Fixing: Secret fix to structure at 1.5m centres with Aluminium Brackets in accordance with Alutec installation guide. Visible fixings to be colour matched.