470 Fascia

Manufacturer: Marley Alutec, Unit 1 (G-H), Hudson Road,
 Elms Farm Industrial Estate, Bedford MK41 0LZ
 Tel: 01234 359438, Fax: 01234 357199.
 Email: enquiries@marleyalutec.co.uk
 Reference: Aluminium composite fascia system
 Profile: Type A

Size: To be determined TBC
 Type / grade: 4mm thick aluminium composite. Polyethylene thermal break between external surfaces

Finish: Kynar 500 fluorocarbon PVDF paint system
 Colour: TBC
 Functional life expectancy: 50 years

Fire resistance: BS476: Part 6 Class 0, BS476: Part 7 Class 1, EN 13501-1 – Class D

Thermal resistance: 0.013m2.KW

Sound insulation: 26dB

Jointing: H-section joint trims

Fixing: Direct fix to structure at 600mm centres